Article

Effect of industrial heat treatment and barrel finishing on the mechanical performance of Ti6Al4V processed by selective laser melting

Filippo Nalli 1, Luana Bottini 2,*, Alberto Boschetto 2, Luca Cortese 2 and Francesco Veniali 2

1	Faculty of Science and Technology, Free University of Bozen-Bolzano, Piazza Università 1, 39100 Bolzano, Italy;

2	Department of Mechanical and Aerospace Engineering. Sapienza Università di Roma, Via Eudossiana 18, 00184, Roma, Italy;

*	Correspondence: luana.bottini@uniroma1.it Tel.: (optional; include country code; if there are multiple corresponding authors, add author initials) +xx-xxxx-xxx-xxxx (F.L.)

Received: date; Accepted: date; Published: date

Abstract: Additive manufacturing is now capable to deliver high-quality, complex-shaped metallic components. The titanium alloy Ti6Al4V is an example of a printable metal being broadly used for advanced structural applications. A sound characterization of static mechanical properties of additively manufactured material is crucial for its proper application, and here specifically for Ti6Al4V. This includes a complete understanding of the influence of post-process treatment on the material behavior, which has not been reached yet.
In the present paper, the post-process effects of surface finish and heat treatment on the mechanical performance of Ti6Al4V after selective laser melting were investigated. Some samples were subjected to barrel finishing at two different intensities, while different sets of specimens underwent several thermal cycles. As a reference, a control group of specimens was included, which did not undergo any postprocessing. The treatments were selected to be effective and easy to perform, being suitable for real industrial applications.
Tensile tests were performed on all the samples to obtain yield stress, ultimate tensile strength and elongation at fracture. The area reduction of the barrel finished samples, after being tested, was measured using a 3D scanner as a further indication of ductility. Experimental results are reported and discussed highlighting the effect of postprocessing treatments on the mechanical response. We then propose the optimal post-processing procedure to enhance ductility without compromising strength for structures manufactured of Ti6Al4V with selective laser melting.

Keywords: Selective Laser Melting; Additive Manufacturing; Ti6Al4V; Barrel finishing; Heat treatment; Tensile test

1. Introduction

Additive manufacturing (AM) technologies are becoming widespread thanks to their promising ability to manufacture nearly any complex shape. The metal additive technologies are extremely attractive, being able to produce structural components, made of the typical metal alloys used in industrial applications. There are a large number of AM methods for metal [1] and can be categorized largely into two groups [2]: Directed Energy Deposition and Powder Bed Fusion. The former is characterized by large process complexity and requires a careful design of the part in order to obtain complex shapes with satisfactory accuracy, thus putting the Directed Energy Deposition at a great disadvantage with respect to powder bed methods. Within the latter category, Selective Laser Melting (SLM) has the ability to produce highly complex-shaped components with relative ease. This being used in several manufacturing areas, ranging from automotive to biomedical, due to its suitability to manufacture light structures, optimizing the material usage. In such a scenario, a complete understanding of the mechanical performance of SLM manufactured parts is crucial, due to the not redundant nature of the AM fabricated structures. The titanium alloy Ti6Al4V is one of the most employed materials in SLM technology and has the following attractive features: high strength, low density as well as excellent corrosion resistance and biocompatibility [3]. Ti6Al4V is a commonly studied alloy and investigations include those to microstructure [4,5], high cycle fatigue [6], static mechanical properties and ductility [7].

Traditional manufacturing processes of Ti6Al4V rely on forging, casting and rolling of bulk feedstock material, followed by machining to final shape and dimensions. These processes suffer disadvantages such as poor machinability of Ti6Al4V as well as high material waste and energy consumption [8,9]. These have begun to steer the industry towards SLM technology. Manufacturing with SLM affects the microstructure in a different way with respect to the traditional manufacturing processes. Because of the high cooling rate, the Ti6Al4V microstructure mainly consists of fine non-equilibrium hcp martensite α’-phase. As a result, the tensile strength of SLM part is higher than that of hot-worked parts, whereas the ductility is lower [10]. In addition, high residual stress usually occurs. A post-processing heat treatment can increase ductility through the transformation of the metastable martensite into a biphasic α-β matrix, resulting in a reduction in strength [11]. Researchers have made great efforts in balancing strength and ductility within SLM fabrication of Ti6Al4V. In [12], the ductility was improved by increasing the baseplate temperature at 570°C, which resulted in less residual stress. In [13], a double scanning at high energy density was employed to obtain fine lamellar α+β microstructure. Although the obtained material performances resulted in improved mechanical behavior, these strategies are not suitable for industrial production because of their lower process efficiency. Hence, the balancing between strength and ductility is to be achieved by subsequent thermal treatment. Depending upon the final requirements, the SLM parts are usually subjected to Hot Isostatic Pressing (HIP) and/or heat treatment operation [14]. The HIP reduces the risk of undesirable porosity and breaks down columnar prior-β grains parallel to the stratification direction, giving a more homogeneous behavior. Recently, most of the efforts aiming to select the best processing parameter set, focused on the relative density and isotropy improving. The Ti6Al4V relative density was improved to 99.99% [15]. Aging thermal treatments are currently the most diffused ways to balance strength and ductility: in [16] and [17] specific heat treatments for SLM Ti6Al4V are mentioned. Nevertheless, the literature mainly focuses on residual stresses, microstructure evolution and fatigue resistance.

The parts manufactured by SLM are prone to a significant amount of induced residual stresses because of the high temperature gradients involved in the process: this phenomenon is amplified in the case of Ti6Al4V due to its poor thermal conductivity. Thus, residual stress increases with the increasing number of layers [18].

Moreover, the scan strategy was proven to have a great influence on the residual stresses: [19] observed the correlation between the scan length and the residual stresses intensity, while [20] observed that residual stresses are larger along the scan direction than the perpendicular one due to the larger thermal gradient. Since residual stresses originate from thermal gradients, the typical way to relieve them after the SLM process is a high temperature stress relief heat treatment [21].

The fatigue properties of as-built Ti6Al4V are similar to those of cast and wrought material, even without a HIP treatment [14]. Obviously, the fatigue life of AM parts increases when surface finishing level is enhanced, since the fatigue is a surface induced critical phenomenon; then AM components need surface finishing operations before service [22].

Thus, the low surface quality is one of the major challenges for AM industrialization. Milling and sandblasting are common solutions, having anyway some drawbacks: SLM products typically have complex geometry thus the geometry freedom is lost when a machining toolpath must be planned, while sandblasting has lower repeatability and surface finishing accuracy, being a manual operation depending on the operator’s skills.

In such a scenario the barrel finishing (BF), which belongs to the family of mass finishing technology, showed improvements of the mechanical performance of SLM parts [23]. It is typically used for finishing operations from radiusing and deburring to very fine finishing. This technique consists in loading a charge composed by the components to be finished, media, water and compound within a rotating barrel: the relative motion between the charge components permits the micro removal of the material performing the finishing operation [24].  The fixturing of the parts during the process is not necessary and therefore it is suitable for components in a variety of sizes, shapes and materials. Moreover, it requires a low investment cost as well as very low maintenance costs [25]. For these characteristics, it is suitable for the finishing of AM parts [26]. The abrasive action is generated by the rotation of the barrel: as the barrel rotates, the charge is moved upwards until the force of gravity overcomes the tendency of the mass to stick together and a layer slides down [27]. Depending on the filling and the rotational speed, six motions take place: sliding, slumping, rolling, cascading, cataracting, and centrifuging [28]. Only two of these motions, i.e. rolling and cascading, permit a continuous flow in a form of avalanches providing the desired soft mechanical action of BF. Hence, adequate process parameters must be chosen. No theoretical model can help in this step because the process parameters strictly depend upon the charge characteristics. The different motions can be described through the bed behavior (BB) diagram which is a map of the attainable motions as a function of the filling percentage and the rotational speed [28]. This BB diagram must be developed experimentally for each charge.

The present study aims to quantify the improvements on the static mechanical properties of SLM Ti6Al4V parts achievable with thermal treatments and BF finishing operation, thus acting both on residual stresses and surface finish quality levels. The specimens were fabricated in three different directions: vertical, horizontal and diagonal. A subset of specimens was subjected to heat treatment with several combinations of temperatures and durations, while another subset underwent BF at various intensities; a third reference subset was not post-processed for a control group. All samples underwent tensile tests to compare the resulting overall mechanical performance and material ductility.

2. Materials and Methods

Ti6Al4V is widely used in a broad range of different applications ranging from use as turbine blades in the aerospace industry to prostheses in the biomedical industry. The employed samples were fabricated via an EOS M290 machine equipped with an Ytterbium laser with a maximum power of 400 W and a building space of 250×250×325 mm3. The SLM technology implies that a laser scans the surface of a powder bed, locally melting the powder alloy, realizing a solid layer when cooling down. The building plate, containing the powder bed, shifts down and a new layer of metallic powder is spread on the top of the just solidified metal and the process goes on, building the component in a bottom-up manner, layer upon layer. The employed Ti6Al4V powder was supplied by EOS GmbH and its chemical composition is reported in Table [1].

Table 1. Chemical composition of Ti6Al4V powder.

| Chemical composition of Ti6Al4V powder [%wt] |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al | V | O | N | C | H | Fe | Y | Ti | Other |
| 5.50-6.75 | 3.50-4.50 | 0.20 | 0.05 | 0.08 | 0.015 | 0.30 | 0.005 | Bal | 0.10 Max |

In Figure 1, a SEM image of the used powders and the granulometry distribution measured by the laser diffraction granulometer Mastersizer 2000 are reported. The particles have a spheroidal shape and d10, d50 and d90 are 23.62 µm, 37.69 µm and 59.11 µm respectively.

Figure 1. (a) SEM image of Ti6Al4V powders; (b) Granulometry distribution of the powders.

All the samples were fabricated adopting the standard process parameters provided by EOS for this alloy. They are summarized in Table [2].

Table 2. Process parameters employed for all samples.

| Process parameters |  |
| --- | --- |
| Layer thickness | 30 µm |
| Laser power | 340 W |
| Focal spot dimension | 0.1 mm |
| Scanning speed | 1250 mm/s |
| Table temperature | 160 °C |
| Hatch spacing | 0.12mm |

The samples geometry employed for the present study is dog-bone, with a square cross-section. Nominal dimensions were chosen according to the standard [29], referring to sintered parts, not being available at present a specific standard for additive manufactured components. The selected geometry has a nominal gauge length of 25.40 mm and a cross-section of 5.72 x 4.00 mm2 (Figure 2).

The first batch of nine specimens was fabricated with three different orientations: vertical, horizontal and inclined of 45° with respect to the building plate. Out of them, 2 sets of 3 specimens (each one with the three different orientations) were processed by 2 different BF conditions; while the remaining 3 samples were not post-processed at all. These first 9 samples were then subjected to tensile tests, showing that this alloy, processed via SLM with the parameters recommended by EOS GmbH, can reasonably be regarded as isotropic. This result was deduced from the overall behavior, represented by the load – displacement curves reported in Fig. 6a, section “Results and discussion”. In the same section, a complete discussion on all the experimental results is presented. The second batch of 30 samples, was afterward fabricated only along the vertical direction using the same process parameters as the first batch; all the specimens were then heat treated with 3 temperatures at different durations (for each heat treatment and heating time three repetitions were tested). Summarizing, overall 39 specimens were studied: 3 were not post-processed, 6 underwent BF and 30 were subjected to heat treatments.

Figure 2. Dog-bone specimen geometry according to the ASTM E8/E8M-04 standard.

The barrel finishing was selected as the surface finishing operation, for its flexibility and easiness to use, while for the heat treatments, different heating cycles were selected, starting from the treatment suggested by the powder supplier [30] and exploring possible alternative towards lower temperatures, to save energy and money in actual applications.

The barrel finishing was carried out using a Rotar EMI 47, an industrial inclined octagonal barrel 400 mm in diameter moved by an asynchronous motor with electronic speed control. The employed media are cylinders are made of a synthetic resin matrix with abrasive consisting of powder of alumina, silica, and silicon carbide. They measure 15 mm in diameter and 25 mm in height and are angled cut (Figure 3a). The rotational speed and the filling percentage were chosen according to the analysis of the Bed Behavior (BB) diagram obtained following the methodology described in [23]. The BB diagram for this experimentation is reported in Figure 3b. The finishing process was performed at two different rotational speeds, in the rolling and cascading domains respectively. Namely, the chosen rotational speeds were 30 rpm and 42 rpm, while the filling percentage of the barrel was set at 50% according to the assessment that at this value the active layer has the greatest surface [31].

Figure 3. (a) Used media; (b) BB diagram for the experimented charge; (c) zoom of the BB diagram and indication of the chosen process parameters

The heat treatment recommended by the M290 EOS material datasheet is 2h at 800°C, while [32] performed an extensive investigation on a broad range of temperatures. Keeping in mind an industrial applicative focus of the study, the authors started from the cycle suggested by EOS GmbH (800°C – 4h) [30], and selected three alternative lower temperatures for the heat treatments: 482°C, 704°C and 788°C. For each one, three heating durations were applied. All the thermal treatments were carried out using a Nabertherm LH120/14 electric furnace at atmospheric pressure.

Table 3 reports all the produced samples, along with their orientation, actual dimensions and the type of applied post-processing. All tensile tests were performed using a servo-hydraulic MTS universal testing machine, capable of a tensile/compressive load up to 250 kN with 150 mm of maximum stroke. Figure 4. shows some details of the experimental setup. All tests were performed under quasi-static loading conditions, imposing a ramped displacement at a run rate of 0.05 mm/min, according to the (ASTM E8/E8M-04) standard. An external extensometer was used, with a base length of 25 mm. Crosshead displacement, axial load and specimen gauge section elongation coming from the extensometer were recorded during runs.

To measure the cross-section reduction and consequently have a qualitative estimation about the ductility, some fractured samples were digitized using a structured light 3D scanner. A GOM Atos Core 300 was employed, being capable of accuracy up to 30 µm, and having a working volume of 300 x 230 x 400 mm3 and a blue light fringes projector, making the acquisition process almost insensitive to ambient light interference.

Figure 4. Experimental set up: (a) universal testing machine; (b) necked specimen just before fracture

| Specimen ID | Gauge section width (W) [mm] | Gauge section thickness (T) [mm] | Fabrication Direction | Heat treatment | Barrel finishing |
| --- | --- | --- | --- | --- | --- |
| BF 00 00 | 5.74 | 4.08 | Horizontal | - | - |
| BF 00 45 | 5.58 | 3.94 | Diagonal | - | - |
| BF 00 90 | 5.54 | 3.77 | Vertical | - | - |
| BF 30 00 | 5.30 | 3.84 | Horizontal | - | 30 rpm |
| BF 30 45 | 5.30 | 3.80 | Diagonal | - | 30 rpm |
| BF 30 90 | 5.40 | 3.64 | Vertical | - | 30 rpm |
| BF 42 00 | 5.30 | 3.80 | Horizontal | - | 42 rpm |
| BF 42 45 | 5.30 | 3.74 | Diagonal | - | 42 rpm |
| BF 42 90 | 5.30 | 3.60 | Vertical | - | 42 rpm |
| TT 482 06 1 | 5.75 | 4.03 | Vertical | 482°C – 6h | - |
| TT 482 06 2 | 5.77 | 4.02 | Vertical | 482°C – 6h | - |
| TT 482 06 3 | 5.76 | 4.06 | Vertical | 482°C – 6h | - |
| TT 482 08 1 | 5.76 | 4.04 | Vertical | 482°C – 8h | - |
| TT 482 08 2 | 5.78 | 4.02 | Vertical | 482°C – 8h | - |
| TT 482 08 3 | 5.77 | 4.08 | Vertical | 482°C – 8h | - |
| TT 482 10 1 | 5.76 | 4.02 | Vertical | 482°C – 10h | - |
| TT 482 10 2 | 5.76 | 4.03 | Vertical | 482°C – 10h | - |
| TT 482 10 3 | 5.79 | 4.03 | Vertical | 482°C – 10h | - |
| TT 704 04 1 | 5.79 | 4.05 | Vertical | 704°C – 4h | - |
| TT 704 04 2 | 5.76 | 4.03 | Vertical | 704°C – 4h | - |
| TT 704 04 3 | 5.79 | 4.04 | Vertical | 704°C – 4h | - |
| TT 704 05 1 | 5.76 | 4.05 | Vertical | 704°C – 5h | - |
| TT 704 05 2 | 5.78 | 4.05 | Vertical | 704°C – 5h | - |
| TT 704 05 3 | 5.80 | 4.03 | Vertical | 704°C – 5h | - |
| TT 704 06 1 | 5.77 | 4.02 | Vertical | 704°C – 6h | - |
| TT 704 06 2 | 5.79 | 4.04 | Vertical | 704°C – 6h | - |
| TT 704 06 3 | 5.76 | 4.04 | Vertical | 704°C – 6h | - |
| TT 788 03 1 | 5.78 | 4.04 | Vertical | 788°C – 3h | - |
| TT 788 03 2 | 5.81 | 4.03 | Vertical | 788°C – 3h | - |
| TT 788 03 3 | 5.80 | 4.02 | Vertical | 788°C – 3h | - |
| TT 788 04 1 | 5.80 | 4.02 | Vertical | 788°C – 4h | - |
| TT 788 04 2 | 5.78 | 3.99 | Vertical | 788°C – 4h | - |
| TT 788 04 3 | 5.78 | 4.03 | Vertical | 788°C – 4h | - |
| TT 788 05 1 | 5.77 | 4.02 | Vertical | 788°C – 5h | - |
| TT 788 05 2 | 5.76 | 4.06 | Vertical | 788°C – 5h | - |
| TT 788 05 3 | 5.79 | 4.03 | Vertical | 788°C – 5h | - |
| TT 800 04 1 | 5.86 | 4.04 | Vertical | 800°C – 4h | - |
| TT 800 04 2 | 5.85 | 4.02 | Vertical | 800°C – 4h | - |
| TT 800 04 3 | 5.87 | 4.01 | Vertical | 800°C – 4h | - |

Table 3. Specimens IDs, actual dimensions and post-processing information.

Each half of the barrel finished samples, after the tensile test, was measured with the scanner, and the resulting point cloud was processed in three subsequent stages. First, the overall 3D geometry was reconstructed (Figure 5a), then multiple cross-sections were isolated along the specimen axis at fixed steps of 0.5 mm using the software GOM Inspect. Afterward, the sections’ perimeters were identified and exported as closed loops, (Figure 5b), and finally post-processed using a MATLAB custom made routine to compute the area enclosed by the loops. Due to the irregular shape of the fracture, the section closest to the fracture (red) was discarded and the next section (green) is considered for surface computation, as schematically shown in Figure 5b.

Figure 5. Example of cross-section measurement using the 3D structured light scanner: (a) acquired and reconstructed 3D shape; (b) cross-sections evaluated through a MATLAB routine.

3. Results

The results of the experimental campaign are reported in the following Figures 6-10. Figure 6 summarizes the overall behavior, in terms of force-displacement curves, of barrel finished and heat-treated samples. For the BF (Figure 6a), only a sample was tested for each combination of building direction and finishing intensity; while for the thermally treated specimens the median value of three repetitions was reported in Figure 6b.

Figure 6. Force – Displacement curves for (a) the barrel finished samples; (b) the heat-treated samples.

Figure 7 shows the corresponding engineering stress-strain curves for barrel finished and heat-treated specimens, respectively, calculated using the actual specimen dimensions measured before the tests.

Figure 7. Stress - Strain curves for (a) the barrel finished samples; (b) the heat-treated samples.

The barrel finished samples exhibited a maximum scatter below 15% in terms of yielding stress, while the thermal-treated specimens showed an improved behavior in terms of repeatability, with the only exception of samples treated at 482°C (TT 482), with a significantly higher yielding value. Their yielding stress, higher than 1050 MPa, resulted to be comparable to that of barrel finished samples, which did not receive any thermal treatment.

Conversely, both the elongation at break and ultimate tensile strength demonstrated a higher scatter due to the influence by the post-processes. Their values are reported in Figure 8a and 9a. In this case, for the heat-treated specimens, the mean values of the three repetitions are used. In Figure 8b and 9b the mean values of ultimate tensile strength, yield stress and elongation at break are summed up for each level of surface finish and each temperature.

Figure 8. (a) Yield stress, ultimate tensile strength and elongation at break of the barrel finished samples; (b) same quantities averaged over the BF speeds.

Figure 9. (a) Yield stress, ultimate tensile strength and elongation at break for the heat-treated samples; (b) same quantities averaged over the post-processing temperature.

Finally, the percentage of area reduction at fracture of the barrel finished specimens, evaluated close to the most critical section, are illustrated in Figure 10.

Figure 10. Area reduction [%] measured with the 3D scanner on fractured samples.

4. Discussion

The tensile tests exhibited a good level of repeatability, in terms of yield stress, elastoplastic behavior, and ultimate tensile strength. Also, the repetitions for each heat-treatment level turned out to be matching perfectly, confirming the consistency of the building and post-conditioning processes. Negligible effects were observed in the mechanical behavior due to fabrication orientation, which essentially excludes the possibility of macroscopic structural anisotropy induced by the production process. Likewise, the surface finish had moderate effects on yielding stress and ultimate tensile strength, with differences below 15% overall. Conversely, the heat-treatments showed a systematic impact both on yield stress and ultimate tensile strength, lowering those values by about 7%. Only the samples cured at 482°C revealed a yield stress comparable to that typical of not treated samples (around 1050 MPa).

All the post-process treatments had a significant influence on the elongation at break. Both the barrel finished samples subsets exhibited an increased fracture elongation of about 25%, while the heat-treatments enhanced the elongation, with respect to their intensity, up to more than 30%. Eventually, the area reduction also showed an increasing trend with the increase of BF velocity.

The influence on the ductility of surface finish condition can be interpreted as the effect of high surface roughness typical of as-built specimens, which might act as a crack initiator. Such roughness, typically in the range of Ra = 5-15 µm [23] can be regarded as a series of superficial defects, causing a stress intensification in some spots on the surface of the sample, which in turn produce a premature fracture. The interpretation is that when the first fracture appears, the stress distribution is not yet the typical one of tensile specimens, in which the critical point, where the deformation should be localized, is known to be the one in the middle of the cross - section. Thus, at fracture onset, the expected critical point, inside, is not more critical than other points on the surface, where conversely the fracture can be triggered by superficial defects causing a local stress intensification.

To support these hypotheses, a numerical simulation of a tensile test was performed to assess the plastic strain at the fracture onset. The simulation was carried out using the commercial finite-element analysis code ANSYS. The material was regarded as isotropic and described with a nonlinear stress-strain law, based on Voce’s formulation. The specimen was discretized using solid elements with quadratic formulation with an average element length of 0.1 mm. All the possible symmetries were exploited in the modeling in order to reduce the number of elements required. Surface roughness and residual stresses were neglected.

The results, reported in Figure 11, show how the total equivalent plastic strain exhibits a nearly homogeneous distribution along the cross-section, showing only a marginal concentration in the inner area. Such behavior suggests that the first failure occurs before reaching a localization of deformation inside the specimen, as observed for instance on standard material. Thus, being inner and outer points of the sample at the same stress level, the fracture is supposed to start outside, triggered by superficial defects or residual stresses.

Figure 11. Total equivalent plastic strain distribution in the specimen at the time of fracture.

Finally, besides the modification of the microstructure, the contribution of heat treatments to ductility enhancement can be explained with the attenuation of residual stresses, induced by the fabrication process. The residual stresses, being manly concentrated on the samples surface, alter the expected stress distribution, hence triggering an untimely fracture onset as for the case of surface roughness.

5. Conclusions

A thorough static mechanical characterization of AM SLM Ti6Al4V was performed, highlighting the influence of different thermal treatments and surface finish on the resulting mechanical performance. Samples were subjected alternatively to BF of different intensities or thermal treatments at different temperatures and durations. Samples were successively subjected to tensile tests under quasi-static conditions. Fracture surfaces and area reduction were additionally evaluated on fractured specimens.

According to experimental evidence, the building direction seemed to not affect the mechanical performance of additive Ti6Al4V significantly, such that the alloy can be reasonably regarded as isotropic. The longer the duration of the heat treatment, the more ductile is the observed material behavior. Analogously, the more intense was the BF, the higher is the elongation at fracture. Both the post-processes can play a key role in the trade-off between strength and ductility having the great advantage of being simple to perform.

The thermal treatments seemed to be more suitable when the ultimate tensile strength is not of primarily importance and a specific microstructure must be obtained. The experimental results pointed out that a temperature of 788°C seemed to be the best choice to increase ductility without compromising strength. On the other hand, BF proved to be effective in enhancing elongation at fracture with a marginal influence on other mechanical properties. Within the two intensities tested in the present work, the one corresponding to 30 rpm rotational speed gave the most beneficial results.

Funding: This research did not receive any specific grant from funding agencies in the public, commercial, or not-for-profit sectors.

Acknowledgments: The authors wish to thank the Dragonfly srl and Eng. Luciano Macera for the specimens’ fabrication.

References

1. 	Milewski, J.O. Additive Manufacturing of Metals; Springer, 2017; ISBN 9783319582047.

2. 	ISO/ASTM 52900 - 15 Standard Terminology for Additive Manufacturing – General Principles – Terminology 2015.

3. 	Donachie, M.J. Titanium: A Technical Guide; ASM International: Metals Park, 1988; ISBN 0.87170-309-2.

4. 	Lütjering, G. Influence of processing on microstructure and mechanical properties of (α+β) titanium alloys. Mater. Sci. Eng. A 1998, 243, 32–45.

5. 	Sieniawski, J.; Ziaja, W.; Kubiak, K.; Motyk, M. Microstructure and Mechanical Properties of High Strength Two-Phase Titanium Alloys. In Titanium Alloys - Advances in Properties Control; 2013.

6. 	Ritchie, R.O.; Davidson, D.L.; Boyce, B.L.; Campbell, J.P.; Roder, O. High-cycle fatigue of Ti-6Al-4V. Fatigue Fract. Eng. Mater. Struct. 1999, 22, 621–631.

7. 	Cortese, L.; Nalli, F.; Broggiato, G.B.; Coppola, T. An effective experimental-numerical procedure for damage assessment of Ti6Al4V. In Proceedings of the Conference Proceedings of the Society for Experimental Mechanics Series; 2016; Vol. 9, pp. 43–49.

8. 	Huang, R.; Riddle, M.; Graziano, D.; Warren, J.; Das, S.; Nimbalkar, S.; Cresko, J.; Masanet, E. Energy and emissions saving potential of additive manufacturing: the case of lightweight aircraft components. J. Clean. Prod. 2016, 135, 1559–1570.

9. 	Lütjering, G.; Williams, J.C. Titanium; 2nd editio.; Springer, 2007; ISBN 978-3-540-71397-5.

10. 	Gu, D. Laser additive manufacturing of high performance materials; Springer, 2015; ISBN 9783662460887.

11. 	Facchini, L.; Magalini, E.; Robotti, P.; Molinari, A.; Höges, S.; Wissenbach, K. Ductility of a Ti-6Al-4V alloy produced by selective laser melting of prealloyed powders. Rapid Prototyp. J. 2010, 16, 450–459.

12. 	Ali, H.; Ma, L.; Ghadbeigi, H.; Mumtaz, K. In-situ residual stress reduction, martensitic decomposition and mechanical properties enhancement through high temperature powder bed pre-heating of Selective Laser Melted Ti6Al4V. Mater. Sci. Eng. A 2017, 695, 211–220.

13. 	Xu, W.; Brandt, M.; Sun, S.; Elambasseril, J.; Liu, Q.; Latham, K.; Xia, K.; Qian, M. Additive manufacturing of strong and ductile Ti-6Al-4V by selective laser melting via in situ martensite decomposition. Acta Mater. 2015, 85, 74–84.

14. 	Dutta, B.; Froes, F.H. Additive Manufacturing of Titanium Alloys: State of the Art, Challenges and Opportunities; Elsevier Inc., 2016; ISBN 9780128047835.

15. 	Kazantseva, N.; Krakhmalev, P.; Yadroitsev, I.; Fefelov, A.; Merkushev, A.; Ilyinikh, M.; Vinogradova, N.; Ezhov, I.; Kurennykh, T. Oxygen and nitrogen concentrations in the Ti-6Al-4V alloy manufactured by direct metal laser sintering (DMLS) process. Mater. Lett. 2017, 209, 311–314.

16. 	ASTM F2924 – 14 Standard Specification for Additive Manufacturing Titanium-6 Aluminum-4 Vanadium with Powder Bed Fusion 2014.

17. 	ASTM F3001 - 14 Standard Specification for Additive Manufacturing Titanium-6 Aluminum-4 Vanadium ELI (Extra Low Interstitial) with Powder Bed Fusion 2014.

18. 	Mercelis, P.; Kruth, J.P. Residual stresses in selective laser sintering and selective laser melting. Rapid Prototyp. J. 2006, 12, 254–265.

19. 	Liu, Y.; Yang, Y.; Wang, D. A study on the residual stress during selective laser melting (SLM) of metallic powder. Int. J. Adv. Manuf. Technol. 2016, 87, 647–656.

20. 	Parry, L.; Ashcroft, I.A.; Wildman, R.D. Understanding the effect of laser scan strategy on residual stress in selective laser melting through thermo-mechanical simulation. Addit. Manuf. 2016, 12, 1–15.

21. 	Liu, S.; Shin, Y.C. Additive manufacturing of Ti6Al4V alloy: A review. Mater. Des. 2018, 164, 107552.

22. 	Chan, K.S.; Koike, M.; Mason, R.L.; Okabe, T. Fatigue life of titanium alloys fabricated by additive layer manufacturing techniques for dental implants. Metall. Mater. Trans. A Phys. Metall. Mater. Sci. 2013, 44, 1010–1022.

23. 	Boschetto, A.; Bottini, L.; Veniali, F. Surface roughness and radiusing of Ti6Al4V selective laser melting-manufactured parts conditioned by barrel finishing. Int. J. Adv. Manuf. Technol. 2018, 94, 2773–2790.

24. 	Boschetto, A.; Bottini, L.; Veniali, F. Microremoval modeling of surface roughness in barrel finishing. Int. J. Adv. Manuf. Technol. 2013, 69, 2343–2354.

25. 	Tulinski, E.H. Mass Finishing in: ASM Metals Handbook vol.5. Surface Engineering 9th edition 1994, 261–277.

26. 	Singh, R.; Singh, M. Surface roughness improvement of cast components in vacuum moulding by intermediate barrel finishing of fused deposition modelling patterns. Proc. Inst. Mech. Eng. Part E J. Process Mech. Eng. 2017, 231, 309–316.

27. 	Gillespie, L.K. Deburring and edge finishing handbook; 1st ed.; Society of Manufacturing Engineers: Dearborne, 1999; ISBN 0872635015.

28. 	Henein, H.; Brimacombe, J.K.; Watkinson, A.P. Experimental study of transverse bed motion in rotary kilns. Metall. Trans. B 1983, 14, 191–205.

29. 	ASTM E8/E8M-04 Standard test methods for tensile testing of metallic materials. Annu. B. ASTM Stand. 2004.

30. 	EOS GmbH Titanium Ti6Al4V - Material Data Sheet EOS M290 2014, 49, 1–5.

31. 	Cotell, C.M.; Sprague, J.A.; Smidt, F.A. ASM Handbook: Vol 05 Surface Engineering; ASM International, 1994; Vol. 5; ISBN 978-0871703842.

32. 	Vrancken, B.; Thijs, L.; Kruth, J.P.; Van Humbeeck, J. Heat treatment of Ti6Al4V produced by Selective Laser Melting: Microstructure and mechanical properties. J. Alloys Compd. 2012, 541, 177–185.

|  | - © 2020 by the authors. Submitted for possible open access publication under the terms and conditions of the Creative Commons Attribution (CC BY) license (http://creativecommons.org/licenses/by/4.0/). |
| --- | --- |